TABLE 5-B

MINIMUM REQUIREMENTS FOR STRUCTURAL

COMPOSITION OF PAVEMENTS

Street

Classification	Flexible Pavements	Rigid Pavements1

MARGINAL	8” Cr. St.		6” P.C.C.

LAND ACCESS	1 1/2” Bituminous Concrete Bind.

Residential	1 1/2” Bituminous Concrete Surf.

LOCAL	8” Cr. St.			6” P.C.C.

Residential	2” Bituminous Concrete Bind.

1 1/2” Bituminous Concrete Surf.

COLLECTOR	8” Cr. St.			7” P.C.C. with Fabric

Residential	3” Bituminous Concrete Base Course	4” Cr. St.

1 1/2” Bituminous Concrete Surf.

LOCAL	8” Cr. St.			7” P.C.C. with Fabric

Commercial and	3” Bituminous Concrete Base Course	4” Cr. St.

Industrial	2” Bituminous Concrete Surf.

COLLECTOR	8” Cr. St.			8” P.C.C.

Commercial and	4” Bituminous Concrete Base Course	4” Cr. St.

Industrial	1 1/2” Bituminous Concrete Bind.

1 1/2” Bituminous Concrete Surf.

1	Joints in rigid pavement shall be in accordance with IDOT BLR 10-4.

ABBREVIATIONS:

Cr. St.		=	Crushed Stone

P.C.C.		=	Unreinforced Portland Cement Concrete